## Slide 1: Overall Organization
CRIPT End-to-End Test Papers
Olsen et al. PPV-b-PI
Synthesis of molecule 1 ((2,5-Di(2′-ethylhexyloxy)toluene))
Reference to Olsen et al.
Synthesis of molecule 2 (2,5-Di(2′-ethylhexyloxy)toluene)
Synthesis of molecule 3 (2′,5′-Di(2′′-ethylhexyloxy)-4′-methyl-N- benzylideneaniline)
Synthesis of poly(phenylene vinylene)
Synthesis of PPVbPI-42
Synthesis of PPVbPI-59
Synthesis of PPVbPI-72
Synthesis of PPVbPI-89
Phase Behavior Study

## Slide 2
Etherification of methylhydroquinone
dissolve, reflux at 80 °C for 1h
methylhydroquinone
KOH
ethanol
Reflux at 80 °C overnight
ethylhexyl bromide
Poured out on water
extracted with ether
clean with column chromatography
2,5-Di(2′-ethylhexyloxy)toluene
Synthesis of molecule 1 ((2,5-Di(2′-ethylhexyloxy)toluene))
NMR diether
diethyl ether

## Slide 3
2,5-Di(2′-ethylhexyloxy)toluene
mixing
chloroform
dimethylformamide
2,5-Di(2′-ethylhexyloxy)-4-methylbenzaldehyde
react below 40 °C, stir for 1h at ambient temperature
refluxed at 80 °C for 48 h
POCl3
Poured out on ice
extracted into dichloromethane, and neutralized
purify with column chromatography
Synthesis of molecule 2 (2,5-Di(2′-ethylhexyloxy)toluene)
water
dichloromethane
NMR aldehyde

## Slide 4
2,5-Di(2′-ethylhexyloxy)-4-methylbenzaldehyde
Reaction at 60 °C under ~10 Torr vacuum for 2h
aniline
2′,5′-Di(2′′-ethylhexyloxy)-4′-methyl-N- benzylideneaniline
Synthesis of molecule 3 (2′,5′-Di(2′′-ethylhexyloxy)-4′-methyl-N- benzylideneaniline)
NMR imine

## Slide 5
2′,5′-Di(2′′-ethylhexyloxy)-4′-methyl-N- benzylideneaniline
Heat to 30 °C, react for 30 min
potassium
tert-butoxide
dimethylformamide
Acidified water and stir for 48h to hydrolyze the unreacted imines
PPV
collect, neutralize product
fractionate with a chromatography column
Synthesis of poly(phenylene vinylene)
water
methanol
NMR PPV
POM PPV
DSC PPV
GPC PPV
Density Column PPV

## Slide 6
Polyisoprene
(PI-42)
Anionic polymerization PI-42
isoprene
benzene
PPV-b-PI-42
sec-butyllithium in cyclohexane
React for 30 min 42
PPV
Terminate remaining PI with butanol 42
Precipitate with methanol 42
Remove homopolymer with column chromatography 42
Polyisoprene
(PI-59)
Polyisoprene
(PI-72)
Polyisoprene
(PI-89)
PPV-b-PI-59
PPV-b-PI-72
PPV-b-PI-89
Synthesis of PPVbPI-42
Synthesis of PPVbPI-59
Synthesis of PPVbPI-72
Synthesis of PPVbPI-89
Terminate remaining PI with butanol 59
Terminate remaining PI with butanol 72
Terminate remaining PI with butanol 89
PPV
PPV
PPV
Anionic polymerization PI-59
Anionic polymerization PI-72
Anionic polymerization PI-89
this is one material that is a mix of two so must be represented as such in the data model
React for 30 min 59
React for 30 min 72
React for 30 min 89
butanol
butanol
butanol
butanol
Precipitate with methanol 59
Precipitate with methanol 72
Precipitate with methanol 89
Remove homopolymer with column chromatography 59
Remove homopolymer with column chromatography 72
Remove homopolymer with column chromatography 89
GPC PI-42
GPC PI-59
GPC PI-72
GPC PI-89

## Slide 7
Phase Behavior Study
SAXS PPV-b-PI-42
PPV-b-PI-42
WAXS PPV-b-PI-42
GPC PPV-b-PI-42
TEM PPV-b-PI-42
1/T Analysis PPV-b-PI-42
Peak Phase ID PPV-b-PI-42
POM PPV-b-PI-42
DPLS PPV-b-PI-42
SAXS PPV-b-PI-59
PPV-b-PI-59
WAXS PPV-b-PI-59
GPC PPV-b-PI-59
TEM PPV-b-PI-59
1/T Analysis PPV-b-PI-59
Peak Phase ID PPV-b-PI-59
POM PPV-b-PI-59
DPLS PPV-b-PI-59

## Slide 8
Phase Behavior Study
SAXS PPV-b-PI-72
PPV-b-PI-72
WAXS PPV-b-PI-72
GPC PPV-b-PI-72
TEM PPV-b-PI-72
1/T Analysis PPV-b-PI-72
Peak Phase ID PPV-b-PI-72
POM PPV-b-PI-72
DPLS PPV-b-PI-72
SAXS PPV-b-PI-89
PPV-b-PI-89
WAXS PPV-b-PI-89
GPC PPV-b-PI-89
TEM PPV-b-PI-89
POM PPV-b-PI-89
DPLS PPV-b-PI-89